UNIZINC™

TECHNICAL

##### DATA SHEET

#### ZINC OXIDE-WHITESEAL

Chemical formula       : ZnO

Molecular Weight       : 81.37

C.A.S.No.                   : 1314-13-2

H.S.Code No.             : 28170010

Sp.Gr.                         : 5.55-5.60

| PROPERTY | UNIT | VALUE |
| --- | --- | --- |
| Zinc Oxide (as ZnO) | % min. | 99.5 |
| Bulk density 1, | gm/cc | 0.55-0.60 |
| Matter soluble in water 4 | % max. | 0.2 |
| Matter insoluble in HCl4 | % max. | 0.05 |
| Loss on Ignition | % max. | 0 .5 |
| Moisture content 2 | % max. | 0.5 |
| Residue through 45µ | % max. | 0.15 |
| Surface area3 | m2/gm | 5-7 |
| PH(2% acq. solution) | -- | 7-7.5 |

- At the time of packing  2) By IR Moisture Balance 3) Determined  on  coulter  SA  3100 Surface Area Analyzer (by Nitrogen adsorption BET method)  4) IS: 7086 (Part I)1973 5) By Anthraquinone  pink spot test

Packing                       : 20 kg

Safety data sheet       : Available on request

Our Rubber Laboratory involved in application research can assist in product development process wherever required.

TM Registered trade mark of Sumit Chemicals Pvt Ltd

Sumit Chemicals (P) Ltd. is an ISO 9001:2000 company & is a group unit of MLA Group of industries INDIA

HEAD OFFICE & R&D CENTRE                                           FACTORY

111/230, HARSH NAGAR,                                                                50, UPTRON ESTATE,

KANPUR (UP)-INDIA                                                                        KANPUR (UP) -INDIA

Tel.:   91 512-2291409, 3099938, 3097073

Fax No. : 91 512-2290057, 2691153

E-mail   : mktg@mlagroup.com  /   sales@mlagroup.com

Website: www.mlagroup.com