|  | ONE-PACK PVC STABILIZER | MLA GROUP |
| --- | --- | --- |
|  | UNISTAB – LPF (Lubricated Flakes) |  |
|  | SUMIT CHEMICALS (P) Ltd., 111/230,HARSH NAGAR,KANPUR Tel. : (0512)-2291408-10, Fax No. : 0512-2290057 E-mail : mlgroup123@rediffmail.com, sales@mlagroup.com |  |

UNISTAB-LPF is a co-precipitate manufactured under controlled conditions, resulting in a high performance heat stabilizer that is better functionally as well as operationally in PVC processing. It is specially designed for Rigid PVC Pipe application and gives excellent results at low as well as high filler loadings.

###### TYPICAL PHYSIOCHEMICAL PROPERTIES

| PROPERTY | UNIT | PP-2 | PP-3 | PP-4 |
| --- | --- | --- | --- | --- |
| Appearance | -- | Snow White to Cream free flowing Powder |
| Metal Content | % | 30-35 | 40-45 | 50-55 |
| Specific Gravity | -- | 2.2-2.4 | 2.3-2.4 | 2.4-2.5 |
| Moisture | % max | 0.5 | 0.5 | 0.5 |
| pH | -- | 6.5-7.5 | 6.5-7.5 | 6.5-7.5 |
| Melting Point | ºC | 105-110 | 105-110 | 105-110 |
| Residue on 240 mesh | % max | 0.5 | 0.5 | 0.5 |
| Free fatty matter | % max | 0.2 | 0.2 | 0.2 |

1) At the time of packing  2) By IR Moisture Balance 3) IS: 7589-1974 (A-8)   4) IS: 12076-1986(A-2)   5) IS: 2850-1983 (A-5.1)

APPLICATIONS:

Rigid PVC Pipes and conduit pipes: The UNISTAB-LPF range of lubricated one pack provides synergistic efficiencies due to their unique proprietary process of manufacture. Use of waxes and calcium stearate is not required separately, as they are self lubricated, although it is at the compounders will depending upon the filler loading and process conditions. The effectiveness increases from LPF-2 to LPF-3 and is the best with LPF-4. Processing requirements as well as commercial criteria are the basis of selection of appropriate grade out of these three. The UNISTAB-LPF range is also unique as it provides ageing resistance to the pipe due to anti-ageing stabilizing component incorporated in the formulation.

This information and our technical advice-whether verbal, in writing or by way of trials are given in good faith but without warranty, and this also applies where proprietary rights of third parties are involved. Our advice does not release you from the obligation to check its validity and to test our products as to their suitability for the intended processes and uses. The application, use and processing of our products and the products manufactured by you on the basis of our technical advice are beyond our control and, therefore, entirely your own responsibility. Our products are sold in accordance with the current version of our General Conditions of Sales and Delivery.